WATERPROOFING SYSTEM

ALSAN TRAFIK HP 500 ZERO

BALCONIES

FOR A COMPLETE DESCRIPTION OF PRODUCTS AND APPLICABLE STANDARDS, PLEASE REFER TO THE TECHNICAL DATA SHEETS (SOPREMA SPECIFICATIONS MANUAL OR WEB SITE WWW.SOPREMA.CA).

PLEASE CONTACT A SOPREMA REPRESENTATIVE TO ASSIST IN THE DESIGN OF SPECIFICATIONS FOR A PARTICULAR PROJECT.

THE ELECTRONIC VERSION OF SOPREMA SPECS IS AVAILABLE ON OUR WEB SITE : WWW.SOPREMA.CA.

# GENERAL

## DESCRIPTION

### This section specifies the requirements for the supply and installation of the elements required for waterproofing and coating of traffic areas, including preparation of surfaces; primer; waterproofing, wear and finishing membranes.

### Waterproofing membrane system: ALSAN TRAFIK HP 500 ZERO by SOPREMA.

## [RELETAED WORK]

### Division [              ] [              ]

## ADDITIONAL WORK TO BE PREFORMED BY THE CONTRACTOR

### [     ]

## TECHNICAL DOCUMENTS

### Submit two (2) copies of the most current technical data sheets. These documents must describe the physical properties of the material, [and explanations about product installation, including installation techniques.]

## CONTRACTOR QUALIFICATIONS

### Coating work shall be performed only by skilled applicators, employed by an installation contractor operating all adequate and necessary equipment to execute such work in accordance with the manufacturer’s recommendations and recognized standards.

## MANUFACTURER’S REPRESENTATIVE

### The coating materials manufacturer may delegate a representative to visit the work site at commencement of work.

### At all times, the contractor shall permit and facilitate access to the site by the manufacturer's representative cited above.

## STORAGE OF MATERIALS

### The materials will be delivered to the work site in the sealed, undamaged original containers.

### The containers must display the lot number and date of manufacture of the product.

### The materials delivered will be carefully stored [in a cool, dry area away from open flames] [and appropriately protected according to the manufacturer’s recommendations].

## QUALITY ASSURANCE AND ENVIRONMENTAL MANAGEMENT

### The coating products manufacturer will provide proof of its ISO 9001 and ISO 14001 certifications.

## WORK SAMPLES

### Produce the work samples required in accordance with section [01 45 00 – Quality control].

### [Complete the first ten square meters] [Perform the equivalent of one day’s work] at the location [indicated] [determined by [the engineer] [the consultant]].  Do not continue the work without obtaining the approval [of the engineer] [of the consultant].

## WARRANTIES

### The coating products manufacturer will provide a written document, issued in the name of the owner, certifying that the products will meet the physical characteristics published by the manufacturer for a period of 5 years beginning at the date of substantial completion of the coating application. No letter from the manufacturer modifying its standard guarantee shall be accepted.  The certificate of guarantee must reflect these requirements.

# PRODUCTS

## PRIMERS

### Description : Two-component polyurethane resin used as a primer on concrete.

#### Characteristics:

##### Colour part A :	Clear

##### Colour part B :	Brownish

##### Viscosity part A (cP) :	250

##### Viscosity part B (cP) :	125

##### Solids content (%) :	> 90%

#### Product specified: ALSAN TRAFIK HP 515 by SOPREMA.

#### OR

### Description : Two-component epoxy primer, used as a fast drying primer, increasing the subsequent adhesion of the ALSAN TRAFIK 500 ZERO system on concrete (slab on grade) and as a vapour barrier when the moisture content of the concrete slab is high.

#### Characteristics:

##### Colour part A :	Yellowish

##### Colour part B :	Amber

##### Viscosity part A (cP) :	400

##### Viscosity part B (cP) :	700

##### Solids content (%) :			97

#### Product specified : ALSAN TRAFIK EP 110  SOPREMA.

## WATERPROOFING MEMBRANE

### Description : Two-component polyurethane resin used as waterproofing membrane.

#### Characteristics:

##### Colour part A :	Amber

##### Colour part B :	Grey

##### Viscosity part A (cP) :	20

##### Viscosity part B (cP) :	7200

##### Solids content (%) :	100

##### Ultimate elongation (%) ASTM D-412 :	> 500

##### Tensile strengh (MPa) ASTM D-412 :	> 4.0

#### Product specified: ALSAN TRAFIK HP 525 by SOPREMA.

## WEAR COAT AND FINISH COAT

### Description : Two-component polyurethane resin, used as wearing course. It is installed in one or more layer depending on the traffic intensity. It is also used as a finish coat.

#### Characteristics:

##### Colour part A :	Grey, dark grey

##### Colour part B :	Yellowish

##### Viscosity part A (cP) :	2200

##### Viscosity part B (cP) :	900

##### Solids content (%) :	100

##### Ultimate elongation (%) ASTM D-412 :	> 100

##### Tensile strengh (MPa) ASTM D-412 :	> 10.0

#### Product specified: ALSAN TRAFIK HP 535 by SOPREMA.

## ACCESSORIES

### AGGREGATE (silica sand): Minimum hardness of 6 on Moh’s scale. Dry with screening at 20 to 30 (mesh).

#### Product specified: [       ].

### CRACK SEALANTS: Polyurethane-based sealant compatible with the coating specified.

#### Product specified: ALSAN ACTIF by SOPREMA.

# EXECUTION

## EXAMINATION AND PREPARATION OF SURFACES

### Surface examination and preparation must be completed in conformance with recommendations in the SOPREMA Specifications Manual.

### Before waterproofing work begins, the owner's representative and the membrane contractor’s foreman will inspect and approve substrate condition and ensure that related work has been properly executed. If necessary, a non-conformity notice will be issued to the contractor so that required corrections can be made.

### The decision to begin application of materials constitutes an implicit acceptance of the surface conditions.

### Do not begin any portion of work until surfaces are dry, free of laitance, curing compounds or other non-adhering particles, in accordance with the manufacturer's instructions and recommendations.

### Before installation of the coating system, the concrete must be cured (at least 28 days) with a minimum hardness of 24MPa (3 500psi).

### The concrete surface must be prepared so that it respects CSP (concrete surface profiles) 2, 3 or 4 of the International Concrete Repair Institute (ICRI). In order to obtain these profiles, grinding is recommended.

### Concrete substrate should have an internal content of 75% RH (ASTM F2170) and a maximum moisture content of 1,5 kg/100m²/24h (ASTM F1869) and to be prepared as required to provide adhesion of the membrane system to substrate with a minimum bond strength of 200psi (1,4MPa) as per CAN/CSA-A23.1-04/A23.2-04 section 6B.

### Cracks of more than 1.6 mm (1/16 of an inch) must be repaired using ALSAN ACTIF.

### If needed, concrete repairs must be done with a mix of ALSAN TRAFIK EP110 and silica fume or with an appropriate product.

## METHOD OF EXECUTION

### Coating work must be executed continuously as surfaces are prepared and weather conditions permit.

### Protect adjacent surfaces against any damage resulting from installation work.

### The coating must not be installed when ambient air temperature or substrate temperature is less than 5°C.  Maintain air temperatures and structural base temperature of traffic topping installation above 5°C for 12 hours before, during and after. Allow pedestrian traffic 24 hours following installation of the system.

### Coating must not be installed in rainy weather or when precipitation is imminent. These instructions are valid for twelve hours before application, during application and for twelve hours after system application.

## EQUIPMENT FOR EXECUTION OF THE WORK

### Maintain equipment and tools clean and in good working order.

## INSTALLATION OF THE CRACK SEALANT COATING

### Fill the cracks using ALSAN ACTIF.

## APPLICATION OF PRIMER (polyurethane)

### Mix each part independently for at least 2-3 minutes.

### Pour part B in the part A back and forth until you have an adequate mix.

### Mix the two parts thoroughly for at least 2 to 3 minutes for a homogeneous consistency.

### Cover the surface with a primer using a roller to reach covering rate.

### Pot life mixing is 50 minutes at 25°C (77°F).

### Once primed, the surface must have a wet look finish. The primer must be completely set before application of the waterproofing membrane (maximum recoat window 36h).

## APPLICATION OF PRIMER (epoxy)

### Pour part B in the part A back and forth until you have an adequate mix.

### Mix the two parts thoroughly for at least1 minute for a homogeneous consistency.

### Cover the surface with a primer using a roller to reach covering rate.

### Pot life mixing is 20-25 minutes at 25°C (77°F).

### The primer must be completely dry before application of the waterproofing membrane (maximum recoat window 3 days).

## INSTALLATION OF THE WATERPROOFING MEMBRANE

### Mix each part independently for at least 2-3 minutes.

### Pour part B in the part A back and forth until you have an adequate mix.

### Mix the two parts thoroughly for at least 2 to 3 minutes for a homogeneous consistency.

### Cover the surface using a roller in order to obtain a wet film thickness of 508 micrometers (20 mils).

### Back roll the surface to level.

### *If there is no need to install the waterproofing layer, apply ALSAN TRAFIK HP 535 over a fully cured ALSAN TRAFIK EP110.

## INSTALLATION OF THE WEAR COAT AND FINISH COAT (pedestrian traffic)

### Mix each part independently for at least 2-3 minutes.

### Pour part B in the part A back and forth until you have an adequate mix.

### Cover the surface using a roller in order to obtain a wet film thickness of 355 micrometers (14 mils).

### While the surface is still wet, back roll with a roller to level. Pot life after mixing is 15 minutes at 25°C (77°F).

### Broadcast aggregates to create a non-slip surface once the installation is completed.

### While the surface is still wet, roll to well encapsulate the aggregates.

Note:  SOPREMA INC. may modify the composition and/or utilisation of its products without prior notice.  Consequently, orders will be filled according to the latest specifications.

- END OF SECTION -