COLD FLUID-APPLIED WATERPROOFING

COLPHENE LM 300

FOR A COMPLETE DESCRIPTION OF PRODUCTS AND APPLICABLE STANDARDS, PLEASE REFER TO THE TECHNICAL DATA SHEETS (SOPREMA SPECIFICATIONS MANUAL OR WEB SITE WWW.SOPREMA.CA).

PLEASE CONTACT A SOPREMA REPRESENTATIVE TO ASSIST IN THE DESIGN OF SPECIFICATIONS FOR A PARTICULAR PROJECT.

THE ELECTRONIC VERSION OF SOPREMA SPECS IS AVAILABLE ON OUR WEB SITE: WWW.SOPREMA.CA.

# General

## DESCRIPTION

### This section specifies the requirements for the supply and installation of the elements required for waterproofing below grade structures.

### Waterproofing system:  Liquid membrane.

## RELATED WORK

### Division [02 40 00] [Demolition and Structure Moving]

### Division [03 00 00] [Concrete]

### Division [04 00 00] [Masonry]

### Division [07 10 00] [Dampproofing and Waterproofing]

### Division [07 21 00] [Thermal Insulation]

### Others: [              ] [              ]

## COMPLEMENTARY WORK TO BE EXECUTED BY THE SUB-CONTRACTOR

## TECHNICAL DOCUMENTS

### Submit two (2) copies of the most current technical data sheets. These documents must describe the physical properties of the material, [and explanations about product installation, including installation techniques, restrictions, limitations and other manufacturer recommendations.]

## CONTRACTOR QUALIFICATIONS

### Waterproofing work shall be performed only by skilled applicators, employed by an installation contractor operating all adequate and necessary equipment to execute such work in accordance with the manufacturer’s recommendations and recognized standards.

## MANUFACTURER'S REPRESENTATIVE

### The waterproofing materials manufacturer may delegate a representative to visit the work site at commencement of work.

### At all times, the contractor shall permit and facilitate access to the site by the manufacturer's representative cited above.

## MATERIALS STORAGE

### Pails of materials should be handled with care and proper equipment.

### Pails of materials shall be carefully stored and adequately protected in accordance with the manufacturer’s recommendations.

## QUALITY ASSURANCE AND ENVIRONMENTAL MANAGEMENT

### The manufacturer of elastomeric bitumen products will provide proof of ISO 9001 and ISO 14001 Certifications.

## WARRANTIES

Note:	If used in combination with SOPREMA’s SOPRADRAIN 10G Drainage Board = 10 years warranty.

### The product manufacturer shall issue a written and signed document in the name of the owner, certifying the product will meet all the physical characteristic published by the manufacturer, for a period of 5  years, starting from the date of completion of installation of membranes. No letter amending the manufacturer’s standard warranty will be accepted and the warranty certificate must reflect these requirements.

# PRODUCTS

## WATERPROOFING COATING

### Description:  Water-based single component rubberised liquid membrane.For applications at temperatures above 2°C only.

### Properties:

#### Film thickness:	Wet – 2.0 mm (80 mil)

#### Dry – 1.0 mm (40 mil)

#### Color:	Red

#### Solids by weight (%):	48

#### Water vapour permeance (ng/Pa·s·m2):	ASTM E96 34 (0.6 perm)

### Specified product: COLPHENE LM 300 by SOPREMA.

## ACCESSORIES

Note:	Specify item below when asphaltic boards are used.

### WATERPROOFING MASTIC

#### Description:  A black, solvent-based mastic containing SBS modified bitumen, fibres and mineral fillers.

#### Specified product:  SOPRAMASTIC by SOPREMA.

Note:	Specify item below when expanded polystyrene insulation is used.

### INSULATON ADHESIVE AND CRACK FILLER COATING

#### Description:  Water-based single component rubberised liquid coating used as insulation adhesive and crack filler. For applications at temperatures above 2°C only.

#### Specified product:  SOPRASEAL LM 200 T by SOPREMA

### PROTECTION BOARD

#### Description: A semi-rigid protection board composed of a mineral fortified asphaltic core formed between two saturated fibreglass felts.

#### Characteristics:

##### Thickness:	3 mm

##### Board size:	Width: [     ] Length: [     ]

#### Specified product: SOPRABOARD by SOPREMA

[OR]

### INSULATION BOARD

#### Description: [Expanded polystyrene insulation] [Extruded polystyrene insulation]

#### Specified product: [             ]

[OR]

### DRAINAGE BOARD

#### Description: Dimpled high-density polyethylene panel.

#### Characteristics:

##### Compressive Strength (kPa):	400 (8400 psf)

##### Roll dimensions:	Width: 2.0 m - Length: 12.5 m

#### Specified product: SOPRADRAIN 10G by SOPREMA.

### TERMINATION BAR

#### Specified product: [             ]

# EXECUTION

## SURFACE PREPARATION

### Surface examination and preparation must be completed in conformance with recommendations in the SOPREMA Specifications Manual.

### Before waterproofing work begins, the owner's representative and the membrane contractor’s foreman will inspect and approve substrate condition and ensure that related work has been properly executed. If necessary, a non-conformity notice will be issued to the contractor so that required corrections can be made. The start of the membrane application will mean that substrate conditions are acceptable for work completion.

### Before commencing work, all surfaces must be smooth, dry, clean and free of ice and debris as per manufacturer’s recommendations.

### No materials will be installed during rain or snowfall.

### Verify the compatibility of all membrane components with curing compounds, coatings or other materials which are already installed on the surfaces to be treated.

### Any cracks over 3 mm wide should be reported. Upon approval from the qualified authority, the crack should be filled in with T grade air/vapour barrier coating. For cracks over 6 mm, a 150 mm (6 inches) wide strip of detail membrane should be installed, centered over the crack.

## METHOD OF EXECUTION

### Work shall be performed on a continuous basis as surface and weather conditions allow.

### Adjoining surfaces shall be protected against any damage that could result from the waterproofing installation.

## EQUIPMENT

### Maintain all equipment and tools in good working order.

## WATERPROOFING COATING INSTALLATION

### The substrate must be clean, solid, and free of debris, grease and any contaminants, which may compromise adhesion.

### COLPHENE LM 300 can be applied by spraying or using a roller. For roller application, anticipate changing the rolls regularly depending on weather conditions.

### Install product as film 2.0 mm (80 mils) thick and measure with wet film gauge.

### Any waterproofing membrane left exposed after backfilling shall be protected from ultra violet and mechanical damages.

Note: Prior to backfilling, it is recommended to protect the waterproofing system with protection boards glued with specified mastic.  Backfilling should commence immediately after installation of protection boards.

## [PROTECTION][INSULATION][DRAINAGE]BOARD INSTALLATION

Note:	Specify item below when asphaltic protection boards are used.

### Apply adhesive with spots 75 mm (3 in) in diameter, every 300 mm (12 in). Bottom panel should be supported or mechanically fixed. On the top row of insulation, apply a continuous bead of adhesive 25 mm (1 in) wide to the top leading edge of the panels to be glued. This bead will protect the adhesive spots during initial cure by limiting the flow of moisture behind the insulation in case of rain.

[OR]

Note:	Specify item below when high density polyethylene drainage boards are used.

### Drape the drainage board and secure without fastening through the waterproofing membrane or tape to the waterproofing membrane.

[OR]

Note:	Specify item below when extruded polystyrene insulation boards are used.

### Apply adhesive with spots 75 mm (3 in) in diameter, every 300 mm (12 in). Bottom panel should be supported or mechanically fixed. On the top row of insulation, apply a continuous bead of adhesive 25 mm (1 in) wide to the top leading edge of the panels to be glued. This bead will protect the adhesive spots during initial cure by limiting the flow of moisture behind the insulation in case of rain.

Note: 	SOPREMA INC. may modify the composition and/or utilisation of its products without prior notice.  Consequently, orders will be filled according to the latest specifications.

-END OF SECTION-