BLOWN INSULATION-

CELLULOSE FIBRES

SOPRA-CELLULOSE

THIS DOCUMENT PROVIDES TECHNICAL INFORMATION REGARDING THE MATERIALS AND INSTALLATION METHODS FOR SOPRA-CELLULOSE AND ACCESSORIES.

FOR A COMPLETE LIST OF TECHNICAL DATA SHEETS, SPECIFICATIONS MANUAL AND DETAILS PLEASE VISIT OUR WEB SITE WWW.SOPREMA.CA

# GENERAL REQUIREMENTS

## DESCRIPTION

### Provide the labour, materials and equipment necessary to complete the installation of cellulose fibre thermal insulation and its accessories as specified on the drawings.

## PERFORMANCE REQUIREMENTS

### Provide cellulose fibre thermal insulation that complies with the requirements of standard CAN/ULC-S703.

### Provide continuity of insulation materials and assemblies in conjunction with materials described in related sections.

## REFERENCES

### CAN/ULC-S703: Standard for Cellulose Fibre Insulation for Buildings.

### CAN/ULC-S102.2: Standard Method of Test for Surface Burning Characteristics of Flooring, Floor, Coverings, and Miscellaneous Materials and Assemblies.

## RELATED WORK

### Division [01 00 00] [General Requirements]

### Division [01 33 00] [Submittals Procedure]

### Division  [05 50 00] [Metal fabrications]

### Division  [06 10 00] [Rough Carpentry]

### Division  [06 17 53] [Shop- Fabricated wood trusses]

### Division [07 21 00] [Thermal Insulation]

### Division [09 29 00] [Gypsum Board]

## SUBMITTALS

### Submit up-to-date technical data sheets from the manufacturer and related documentation for the insulation used.

### Submit samples of the insulation material specified in Section 01 33 00- Documents/ Samples to be submitted.

### Submit shop drawings in accordance with Section 01 33 00- Documents/ Samples to be submitted. The shop drawings shall contain a description of the materials.

## CONTRACTOR QUALIFICATIONS

### The work described in this section shall be performed by a competent subcontractor with at least two years experience and trained [and certified] installer for the installation of products, systems and assemblies of this section.

### Installation shall comply with the manufacturer’s installation instructions.

## MANUFACTURER'S REPRESENTATIVE

### The contractor shall at all times permit and facilitate jobsite access to any representative of the insulation manufacturer.

## MATERIALS STORAGE

### Materials shall be delivered in original packaging with the manufacturer’s information and the Material Safety Data Sheet.

### Handle materials with proper equipment.

### Store materials in its original packaging, protected from direct sunlight, moisture and deterioration.

## QUALITY ASSURANCE AND ENVIRONMENTAL MANAGEMENT

### Supply thermal cellulose insulation and accessories from one manufacturer to ensure total system compatibility and integrity.

### Manufacturing facilities of thermal cellulose insulation products to be ISO certified.

## WARRANTIES

### The product manufacturer shall issue a written and signed document in the name of the owner, certifying the product will meet all the physical characteristic published by the manufacturer, for a period of  5 years, starting from the date of completion of installation of insulation. No letter amending the manufacturer’s standard warranty will be accepted and the warranty certificate must reflect these requirements.

# PRODUITS

## BASIS OF DESIGN :

### SOPREMA CANADA INC

### 1688 Jean-Berchmans-Michaud

### Drummondville, QC, J2C 8E9

### Web site : www.soprema.ca

## CELLULOSE FIBRES INSULATION

### Insulation is made of 85% post-consumer recycled newspaper, odourless and  low VOC content, used to reduce the transmission of heat and sound in walls, floors and attics.

### Properties :

#### Colour :  			Grey

#### Thermal resistance (per inch):			R=3.7 RSI=0.65

#### Flame spread rating :

#### CAN/ULC-S102.2			< 150

#### Smoke developed classification			< 45

#### Open-flammability (W/cm²) :			≥ 0.12

#### Open-flammability permanency (W/cm²) :			≥ 0.12

#### Smoulder resistance (% of mass loss): 			≤ 15

#### Moisture vapour sorption (% of mass gain) :			≤ 20

#### Separation of chemicals (% of mass) :	 		≤ 1.5

#### Fungi resistance : 			No growth

### Specified product : SOPRA-CELLULOSE by SOPREMA.

## ACCESSORIES MATERIALS

### RULER

#### Ruler to control and verify the thickness of cellulose fiber insulation in the attic.

#### Specified product : SOPRA-CELLULOSE RULER by SOPREMA

### AERATION VENT

#### Rigid prefolded cardboard piece perforated along fold lines, used to prevent the cellulose insulation from spilling into the roof overhang during installation.

#### Specified product : SOPRA-CELLULOSE VENT by SOPREMA.

### SELF-ADHESIVE PATCH FOR RESTRAINT MEMBRANE

#### Self-adhesive patch which closes the injection holes in the restraint membrane after cellulose fibre insulation has been applied in the walls, the floors and the ceilings.

#### Specified product : SOPRA-CELLULOSE PATCH by SOPREMA.

### CARDBOARD STRIP FOR SECURING THE RESTRAINT MEMBRANE

#### Cardboard strip affixed to the uprights and crosspieces to secure the restraint membrane for injection of the cellulose fibre insulation.

#### Specified product : SOPRA-CELLULOSE STRIP by SOPREMA.

# EXECUTION

## EXAMINATION AND PREPARATION OF SURFACES

### Make sure that the area is well ventilated before installing the insulation.

### Check that there is no obstruction of the void space within the walls before installing the insulation.

### Check that the joints of the support panels attached to the uprights are perfectly butted together before installing the insulation.

## INSTALLATION OF THE INSULATION IN THE ATTIC

### Secure aeration vents between the roof trusses before placing the insulation. Leave at least 1 1/2” (38 mm) space for air circulation in the ventilated roof between the vents and the roof deck.

### Secure the truss rulers with the numbering facing the access hatch. The bottom of the ruler must be installed at the same level as the bottom of the insulation.

### Install the insulation by pneumatic blowing in the roof space between the roof joists in order to obtain a layer of insulation with regular density and thickness in accordance with the manufacturer’s attic coverage chart.

### Leave clearance between the top of the insulation and the underside of the roof deck in accordance with the National Building Code of Canada in force.

### Stop the insulation at least 3” (75 mm) from any heat-emitting elements and chimneys.

### Attach the attic coverage chart prepared by Soprema on a roof truss next to the access hatch, duly signed by the person in charge of the thermal insulation work.

## INSTALLATION OF THE INSULATION IN WALLS

### Supply and install a restraint membrane on the studs with cardboard strips and staples. The membrane must be installed free of all wrinkles.

### Make an opening in the restraint membrane at about two-thirds of the height of the wall.

### Inject the dry insulation in the wall between the studs using a preapproved nozzle and obtain the minimal density recommended :

### 56 kg / m³ (3.5 lb / ft³) for structures of 38 mm x 150 mm (2 x 6 inches) and less

### 64 kg / m³ (4 lb / ft³) for structures greater than 38 mm x 150 mm (2 x 6 inches)

### Finish by installing the self-adhesive patch for restraint membrane to close the opening.

## INSTALLATION OF THE INSULATION IN FLOORS/ CEILINGS

### Supply and install a restraint membrane on the floor or ceiling joists with staples. The membrane must be installed free of all wrinkles.

### Install resilient furring strips or bars every 16” (406 mm) o.c. on the restraint membrane.

### Make an opening in the restraint membrane and inject the dry insulation between the floor or ceiling joists using a preapproved insulating needle to obtain the density recommended: between 28.8 kg/m³ (1.8 lb / ft³) and 48 kg/m³ (3.0 lb / ft³).

### When continuity of the vapour barrier is required, finish by installing the self-adhesive patch for the restraint membrane on the opening of the restraint membrane.

## PROTECTION AND CLEANING

### Protect all the other parts of the work during performance of the job.

### Repair all damaged parts of the work to the architect’s satisfaction.

### When the insulation work is finished, remove all surplus insulation material and waste from the site.

### Note: 	SOPREMA INC. reserves the right to make changes to this specification and associated details without prior notice.

- END OF SECTION -