## PART 1 – GENERAL

  - Section Includes

- Sprayed cellulose finish system.

  - Related Items

- Clips, hangers, supports, sleeves and other attachments to spray bases are to be placed by other trades prior to the application of sprayed insulation.

- Ducts, piping, conduit or other suspended equipment shall not be positioned until after the application of sprayed insulation.

  - Submittals

- Copy of manufacturer’s ISO 9001:2015 Certification.

- Submit 2 copies of test reports indicating compliance with the following:

- Minimum light reflectivity:

  - Arctic White:  81+

  - White:  73+

- NRC values per ASTM C-423 conducted by a NVLAP certified testing laboratory:

| SonaSpray “fc” on Solid Backing |
| --- |
| Inches | 125 HZ | 250 HZ | 500 HZ | 1000 HZ | 2000 HZ | 4000 HZ | NRC |
| 0.50” | .00 | .14 | .49 | .87 | 1.00 | .99 | .65 |
| 0.75” | .10 | .23 | .70 | .98 | 1.01 | .96 | .75 |
| 1.00” | .05 | .40 | .94 | 1.04 | .97 | .99 | .85 |
| SonaSpray “fc” on Ribbed Metal Deck |
| Inches | 125 HZ | 250 HZ | 500 HZ | 1000 HZ | 2000 HZ | 4000 HZ | NRC |
| 0.75” | .17 | .58 | .91 | .89 | .87 | .84 | .80 |

3.	Flame Spread Index:  5	ASTM E-84/UL 723

4.	Smoke Developed:     5	ASTM E-84/UL 723

#### 5.	Bond Strength

SonaSpray “fc”		>600 psf ASTM E-736

SonaSpray “fc” Dura-K	>900 psf ASTM E-736

#### 6.	Compression Strength

SonaSpray “fc”		>400 psf ASTM E-761

SonaSpray “fc” Dura-K 	>600 psf ASTM E-761

7.  Comply with 2009 Section IBC 803.10 stability requirements for interior finishes.

- Manufacturer’s written certification that product contains no asbestos, fiberglass or other man-made mineral fibers.

  - Quality Assurance

- Manufacturer must have a current listing with Underwriters Laboratories (UL) Code Evaluation Report.

- Manufacturer must be in compliance with the 2009 and 2012 International Building Code.

- Manufacturer must be ISO 9001:2015 Certified.

- Applicator:  Licensed by manufacturer.

- Manufacturer must subscribe to independent laboratory follow-up inspection services of Underwriters Laboratories.  Each bag shall be labeled accordingly.

- Mock-up:  Apply a 100 square foot representative sample to be reviewed by the Architects and/or Owner prior to proceeding.

1.05 Delivery, Storage and Handling

- Deliver in original, unopened containers bearing name of manufacturer, product identification and reference to U.L. testing.

- Store materials dry, off ground and under cover.

- Protect liquid adhesive from freezing.

PART 2 – PRODUCTS

  - Acceptable Manufacturers

- International Cellulose Corporation

12315 Robin Boulevard

Houston, Texas 77045

(713) 433-6701 or (800) 444-1252

Distributor :

SOPREMA

1688, Jean-Berchmans-Michaud street

Drummondville (Quebec)  J2C 8E9

1-877-MAMMOUTH

- For approved applicators contact SOPREMA at 1-877- MAMMOUTH.

  - Materials (Specify desired product)

- SonaSpray “fc” Acoustical Finish (4:1 Adhesive Ratio)

- SonaSpray “fc” Dura-K (3:1 Adhesive Ratio)

C.   Color shall be _________________________.

PART 3 – EXECUTION

  - Examination

- Examine surfaces and report unsatisfactory conditions in writing.  Do not proceed until unsatisfactory conditions are corrected.

- Verify surfaces to receive spray insulation to determine if priming/sealing (water based primer, ex. : Iso-Prime) is required to ensure bonding and/or to prevent discoloration caused by migratory stains.

  - Preparation

- Provide masking, drop cloths or other satisfactory coverings for materials/surfaces that are not to receive insulation to protect from over-spray.

- Coordinate installation of the sprayed cellulose fiber with work of other trades.

- Prime surfaces as required by manufacturer’s instructions or as determined by examination.

  - Installation

- Average thickness to achieve NRC of 0.65 or greater.

- Install spray applied acoustical finish according to manufacturer’s recommendations.

- Cure material with continuous natural or mechanical ventilation.

- Remove and dispose of over spray.

  - Protection

- Protect finished installation under provisions of Division 1.

# END OF SECTION