LIQUID-APPLIED WATERPROOFING SYSTEM

FOR BALCONIES, PEDESTRIAN GATEWAY AND OTHER LIGHT PEDESTRIAN TRAFFIC

ALSAN LIGHT TRAFIK ZERO

THIS DOCUMENT PROVIDES TECHNICAL INFORMATION REGARDING THE MATERIALS AND INSTALLATION METHODS FOR LIQUID-APPLIED WATERPROOFING SYSTEM FOR BALCONIES, PEDESTRIAN GATEWAY AND OTHER LIGHT PEDESTRIAN TRAFFIC AND ACCESSORIES.

FOR A COMPLETE LIST OF TECHNICAL DATA SHEETS, GUIDE SPECIFICATIONS AND DETAILS PLEASE VISIT OUR WEB SITE WWW.SOPREMA.CA

# GENERAL REQUIREMENTS

## DESCRIPTION

### Supply labour, materials, and equipment to complete the installation of the liquid-applied waterproofing system for balconies, pedestrian gateway and other light pedestrian traffic including surface preparation and accessories.

### The guidelines in this document should be read in conjunction with the product data sheets.

### Liquid-applied waterproofing system: ALSAN LIGHT TRAFIK ZERO by SOPREMA.

## PERFORMANCE REQUIREMENTS

### Install the system so as to accommodate movements of building elements and materials.

### Ensure the continuity of waterproofing materials and pre-applied assembly in conjunction with materials described in related sections.

## REFERENCES

### ASTM C1305 : Standard Test Method for Crack Bridging Ability of Liquid-Applied Waterproofing Membrane

### ASTM D412: Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers—Tension

### ASTM D570 : Standard Test Method for Water Absorption of Plastics.

### ASTM D624: Standard Test Method for Tear Strength of Conventional Vulcanized Rubber and Thermoplastic Elastomers

### ASTM D2240: Standard Test Method for Rubber Property—Durometer Hardness

### ASTM D2369: Standard Test Method for Volatile Content of Coatings

### ASTM D5895 : Standard Test Methods for Evaluating Drying or Curing During Film Formation of Organic Coatings Using Mechanical Recorders.

### ASTM D7234: Standard Test Method for Pull-Off Adhesion Strength of Coatings on Concrete Using Portable Pull-Off Adhesion Testers

### ASTM E96 : Standard Test Methods for Water Vapor Transmission of Materials

### CAN/CSA-A23.1-04/A23.2-04 SECTION 6B: Concrete materials and methods of concrete construction/Test methods and standard practices for concrete

## RELATED WORK

### Division [03 00 00] [Concrete]

### Division [05 00 00] [Metal]

### Division [07 00 00] [Thermal and moisture protection]

## SUBMITTALS

### Submit manufacturers’ current product data sheets for the components of specified liquid-applied waterproofing membrane system.

## CONTRACTOR QUALIFICATIONS

### Works described in this section must be carried out by a competent contractor certified in waterproofing, employed by a company having the adequate experience and equipment necessary for the works described in this document.

## MANUFACTURER'S REPRESENTATIVE

### The coating materials manufacturer may delegate a representative to visit the work site at commencement of work.

### The contractor shall at all times permit and facilitate job site access to any representative of the cold fluid-applied waterproofing materials manufacturer.

## STORAGE OF MATERIALS

### Handle materials with proper equipment.

### The materials will be delivered to the work site in the sealed, undamaged original containers.

### The containers must display the lot number and date of manufacture of the product.

### The materials delivered will be carefully stored [in a cool, dry area away from open flames] [and appropriately protected according to the manufacturer’s recommendations].

## QUALITY ASSURANCE AND ENVIRONMENTAL MANAGEMENT

### Supply liquid-applied waterproofing membrane components (including accessories) from one membrane manufacturer to ensure total system compatibility and integrity.

### The liquid-applied waterproofing products manufacturer will provide proof of its ISO 9001 and ISO 14001 certifications.

## WARRANTIES

### The product manufacturer shall issue a written and signed document in the name of the owner, certifying the product only will meet all the physical characteristic published by the manufacturer, for a period of 5 years, starting from the date of completion of the installation of liquid membranes. No letter amending the manufacturer’s standard warranty will be accepted and the warranty certificate must reflect these requirements. Since application methods and site conditions are beyond our control and may affect system performance, SOPREMA only guarantees material failure.

# PRODUCTS

## BASIS OF DESIGN:

### SOPREMA CANADA INC

### 1688 Jean-Berchmans-Michaud

### Drummondville, QC, J2C 8E9

### Web site: www.soprema.ca

## LIQUID-APPLIED WATERPROOFING MEMBRANE

### Two-component, VOC-free, odourless, and 100%-solids polyurethane resin.

#### Properties:

##### Colour part A:	White

##### Colour part B:	Amber

##### Viscosity part A (cP):	2 700

##### Viscosity part B (cP):	600

##### Solids content (%):	100

##### Bond strength (MPa) ASTM D7234: 	> 2.0

##### Elongation at break (%) ASTM D-412:	150

##### Tensile strength (MPa) ASTM D-412 :	> 5

##### Water absorption, 24h (%) ASTM D570 :	0.3

##### VOC content (g/l) ASTM D2369 : 	< 6

##### Crack Bridging ASTM C1305 :	Pass

##### Water vapour permeability (perms) ASTM E96 :0.3

##### Hardness (Shore A) ASTM D2240 :	75-80

##### Fully cured, @ 22 °C 50% RHASTM D5895 : 8hrs

#### Product specified: ALSAN TRAFIK PU 221 by SOPREMA.

## WEAR COAT

### Two-component polyurethane aliphatic resin, used as wearing course. It is installed in one or more layer depending on the traffic intensity. It is also used as a finish coat.

#### Properties:

##### Colour part A:	Grey, dark grey

##### Colour part B:	Clear

##### Viscosity part A (cP):	2200

##### Viscosity part B (cP):	900

##### Solids content (%):	100

##### Ultimate elongation (%) ASTM D-412:	120

##### Tensile strength (MPa) ASTM D-412:	> 10.0

##### Bond strength (MPa) CAN/CSA-A23.1-04: 	> 1.4

##### Hardness (Shore A) ASTM D-2240:	95

##### Fully cured, @ 20 °C 50% RH: 		9h

#### Product specified: ALSAN TRAFIK HP 535 by SOPREMA.

## ACCESSORIES

### PRIMERS

#### Two-component epoxy resin used as a primer on concrete.

#### Properties:

##### Colour part A:				Clear or translucent white

##### Colour part B:				Yellowish

##### Viscosity part A (cP):			870

##### Viscosity part B (cP):			2150

##### Solids by weight (%):			100

##### Bond strength (MPa):			> 2

##### Fully cured, @ 20 °C 50% RH: 	3-4h

#### Specified product: ALSAN FLOOR EP 101 by SOPREMA.

### [OR]

#### Two-component polyurethane resin used as a primer on concrete.

#### Properties:

##### Colour part A:	Clear

##### Colour part B:	Brownish

##### Viscosity part A (cP):	250

##### Viscosity part B (cP):	125

##### Solids content (%):	100 %

##### Bond strength (MPa):				3

##### Fully cured, @ 20 °C 50% RH: 		2-3h

#### Specified product: ALSAN TRAFIK HP 515 by SOPREMA.

### CRACK SEALANT

#### Adhesive sealant made of moisture cure polyether, with solvent free, low VOC and isocyanates free. Application temperature must be above 0 °C.

#### Product specified: SOPRASEAL SEALANT by SOPREMA.

### AGGREGATES (silica sand)

#### Minimum hardness of 6 on Moh’s scale. Dry with screening at 20 to 26 (mesh).

#### Specified product: [       ]

### CLEANER

#### Clear blenched solvent used to clean and reactivate the transition area of in-place rapid-curing.

#### Specified product: ALSAN RS CLEANER by SOPREMA

# EXECUTION

## EXAMINATION AND PREPARATION OF SURFACES

### The following conditions must be met regarding the examination and preparation of surfaces: do not begin any work until surfaces are dry, and free of ice, oil, grease, dirt, excess mortar, or other contaminants. Abrasion of the surface is required to remove contaminants. Do not use liquid products to remove contaminants. Fill in damaged surfaces before application system.

### Before waterproofing work begins, the owner's representative and the membrane contractor’s foreman will inspect and approve substrate condition and ensure that related work has been properly executed. If necessary, a nonconformity notice will be issued to the contractor so that required corrections can be made.

### The decision to begin application of materials constitutes an implicit acceptance of the surface conditions.

### The curing period of the concrete must be at least twenty-eight (28) days with a minimum compressive strength of 24 MPa (3,500 psi); concrete must be free of voids.

### Prepare the concrete to obtain a surface profile (ICRI CSP) of 3 or 4. Use special equipment to achieve such a profile. Shot blasting is recommended.

### Concrete substrate should be prepared as required to provide proper adhesion of the membrane system to the substrate with a minimum bond strength of 1.4 MPa (200 psi) as per CAN/CSA-A23.1-04/A23.2-04 section 6B (or ASTM D 7234).

### The moisture content of the concrete must be measured and must be less than or equal to 4 % when measured with a TRAMEX CME4 according to ASTM F2659, or less than 1.5 kg / 100 m² / 24 h when measured according to the ASTM F1869 method.

### Remove release agents or other contaminants from the surface of the concrete substrate; use an approved cleaning agent, such as isopropyl alcohol, to remove them completely.

### Cracks of more than 1.6 mm (1/16 of an inch) must be repaired using crack sealant.

### All upstands (walls, columns, etc.) must also be prepared with crack sealant.

### If needed, concrete repairs must be done with a mix of epoxy primer and silica fume or with an appropriate product.

### The liquid-applied waterproofing membrane cannot be installed without a primer if the substrate does not meet all of the previous conditions. Additional testing may be required by an external consultant depending on the condition of the substrate. A test patch is required on an area of 1 m x 1 m before proceeding with the main application.

## EXECUTION METHOD

### Waterproofing system work must be executed continuously as surfaces are prepared and weather conditions permit.

### Protect adjacent surfaces against any damage resulting from installation work.

### The waterproofing system must not be installed when ambient air temperature or substrate temperature is less than 10 °C. Maintain air temperatures and structural base temperature of traffic topping installation above 10 °C for 12 hours before, during and after. Allow pedestrian traffic 24 hours following the installation of the system.

### Waterproofing system must not be installed in rainy weather or when precipitation is imminent. These instructions are valid for twelve hours before application, during application and for twelve hours after system application.

## EQUIPMENT

### Maintain equipment and tools clean and in good working order.

## APPLICATION OF POLYURETHANE PRIMER

### Stir the contents of Part A and Part B separately for 2 to 3 minutes. Add Part B to Part A, making sure to incorporate the entire contents.

### Mix thoroughly for at least 2 to 3 minutes with a low-speed mixer (300–450 rpm) and a “Jiffy” type mixing paddle in order to ensure a homogeneous consistency.

### Immediately pour the mixture onto the substrate and cover the surface with a primer using a roller or a flat squeegee squeegee to obtain a wet film thickness of 203 à 254 micrometres (8 à 10 mils).

### Note: Pot life mixing is 50 minutes at 25 °C (77 °F).

### Note: The primer must be completely set before application of the waterproofing membrane (maximum recoat window of 36 h).

## APPLICATION OF EPOXY PRIMER

### Pour part B in the part A back and forth until you have an adequate mix.

### Mix the two parts thoroughly for at least1 minute for a homogeneous consistency.

### Cover the surface using a roller or a flat squeegee to obtain a wet film thickness of 254 micrometres (10 mils).

### Note: The primer must be dry to the touch before applying the self-levelling coat (maximum time to apply the next coat is 72 hours).

## APPLICATION OF THE WATERPROOFING MEMBRANE

### Stir the contents of Part A and Part B separately for 2 to 3 minutes. Add Part B to Part A, making sure to incorporate the entire contents.

### Mix Part A and Part B together for 2 to 3 minutes to obtain a homogeneous consistency and immediately pour the mixture onto the substrate.

### Cover the surface using a 4.7 mm (3/16 in) notched squeegee in order to obtain a wet film thickness of 635 micrometres (25 mils). The waterproofing membrane will become completely opaque when the thickness of 25 mils is reached.

### Back roll the surface to level.

### Note: If there is no need to install the waterproofing layer, apply finish coat over a fully cured primer.

## APPLICATION OF THE WEAR COAT

### Stir the contents of Part A and Part B separately for 2 to 3 minutes. Add Part B to Part A, making sure to incorporate the entire contents

### Mix thoroughly both parts for at least 2 to 3 minutes with a low speed mixer (300 to 450 rpm) and a “Jiffy” type mixing paddle in order to ensure a homogeneous consistency; immediately pour the mix on the substrate.

### Cover the surface using a roller in order to obtain a wet film thickness of 355 micrometres (14 mils) (maximum recoat window of 36 h).

### Spread aggregates to create a non-slip surface once the installation is completed.

### While the surface is still wet, roll to well encapsulate the aggregates.

### Note: Pot life after mixing is 15 minutes at 25 °C (77 °F).

### Note: It is necessary to wait 72 hours after the application of the finish coat before traffic can travel over the surface. Provide and install temporary barriers to protect the membrane during the setting period.

## INSPECTION

### Inspect the entire liquid-applied waterproofing membrane at the end of the works before carrying on with the covering work. Any imperfections must be repaired.

## CLEANING AND PROTECTION

### The applicator shall protect the liquid-applied waterproofing system from damage during its installation. The general contractor shall make provisions to protect the liquid-applied waterproofing during the remainder of the construction period. Repair any damage that may occur after application.

### Remove protective materials after application.

### Clean and remove daily all waste and debris from the worksite to avoid damage and operation disruption.

### Clean tools with a specified cleaner. Refer to the manufacturer’s recommendations for spray equipment cleaning.

Note: 	SOPREMA INC. reserves the right to make changes to this specification and associated details without prior notice.

- END OF SECTION -