LIQUID-APPLIED WATERPROOFING COATINGS FOR VEHICLE TRAFFIC AREAS

ALSAN TRAFIK RS

THIS DOCUMENT PROVIDES TECHNICAL INFORMATION REGARDING THE MATERIALS AND INSTALLATION METHODS FOR COATINGS FOR CAR TRAFFIC AREAS MADE OF PMMA AND ACCESSORIES.

FOR A COMPLETE LIST OF TECHNICAL DATA SHEETS, GUIDE SPECIFICATIONS AND DETAILS PLEASE VISIT OUR WEB SITE WWW.SOPREMA.CA

# GENERAL REQUIREMENTS

## DESCRIPTION

### Supply labour, materials, and equipment required to complete the installation of the entire coating system for car traffic areas made of PMMA specified in this section, including surface preparation and accessories.

### PMMA waterproofing system: ALSAN TRAFIK RS by SOPREMA.

## PERFORMANCE REQUIREMENTS

### Install waterproofing system to accommodate movements of the materials and structural elements in place.

### Ensure the continuity of waterproofing materials and assemblies of PMMA-based systems in accordance with the materials described in the related sections.

## REFERENCES

### ASTM D2240: Standard Test Method for Rubber Property—Durometer Hardness

### ASTM D4060: Standard Test Method for Abrasion Resistance of Organic Coatings by the Taber Abraser

### ASTM D562: Standard Test Method for Consistency of Paints Measuring Krebs Unit (KU) Viscosity Using a Stormer-Type Viscometer

### ASTM D1475: Standard Test Method for Density of Liquid Coatings, Inks, and Related Products

## RELATED WORK

### Division [01 00 00] [General Requirements]

### Section [01 33 00] [Submittals Procedure]

### Section [03 01 00] [Maintenance of Concrete]

### Section [03 30 00] [Cast‐in‐place concrete]

### Section [03 31 00] [Structural concrete]

### Section [03 35 00] [Concrete Finishing]

### Section [03 39 00] [Concrete Curing]

### Section [07 90 00] [Protection joint]

## SUBMITTALS

### Submit manufacturers’ current product data sheets for the components of specified PMMA system.

### Submit colour samples on rigid substrate for approval by the Owner, Architect or Engineer specified in Section 01 33 00 ‒ Documents/Samples to Be Submitted.

## CONTRACTOR QUALIFICATIONS

### Works described in this section must be carried out by a competent contractor certified in PMMA-based waterproofing, employed by a company having the adequate experience and equipment necessary for the works described in this document.

## MANUFACTURER’S REPRESENTATIVE

### The waterproofing materials manufacturer may delegate a representative to visit the work site at commencement of work.

### The contractor shall at all times permit and facilitate jobsite access to any representative of the liquid-applied waterproofing materials manufacturer.

## STORAGE OF MATERIALS

### The materials will be delivered to the work site in the sealed, undamaged original containers.

### The containers must display the lot number and date of manufacture of the product.

### The delivered materials will be carefully stored and adequately protected according to the manufacturer’s recommendations in order to prevent deterioration caused by humidity, heat, direct sunlight, or any other source.

### Ensure storage areas housing coating materials are above 0 °C (32 °F) and below 25 °C (77 °F).

## QUALITY ASSURANCE AND ENVIRONMENTAL MANAGEMENT

### Supply all coats of coating systems (including related components and accessories) from a single coating manufacturer to ensure complete system compatibility and integrity.

### The coating products manufacturer will provide proof of its ISO 9001 and ISO 14001 certifications.

## WORK SAMPLES

### A sample of at least 2 m2 (20 ft2) representative of each system must be taken on site, reviewed and accepted by all parties before commencing any work. The sample will serve as a guide for the installation of each system in the entire project.

## WARRANTIES

### The product manufacturer shall issue a written and signed document in the name of the owner, certifying the product will meet all the physical characteristic published by the manufacturer, for a period of 5 years, starting from the date of coating application for car traffic areas. No letter amending the manufacturer’s standard warranty will be accepted and the warranty certificate must reflect these requirements.

# PRODUCTS

## BASIS OF DESIGN:

### SOPREMA CANADA INC

### 1688 Jean-Berchmans-Michaud

### Drummondville, QC, J2C 8E9

### Web site: www.soprema.ca

## WATERPROOFING MEMBRANE

### Two-component polymethyl methacrylate-based (PMMA) liquid membrane is combined with fleece fabric to form a self-adhering reinforced field membrane.

### Properties:

##### Peak load at 23 °C (73 °F) (kN/m):				12.3

##### Elongation at peak load (%):					42

##### Peak load at 23 °C (73 °F) (kN/m):				15.8

##### Elongation at peak load (%):					55

##### Shore A hardness:						81

##### Water absorption, (Method I) (24 h at 23 °C [73 °F]) (%):	0.41

##### Water absorption, (Method II) (48 h at 50 °C [122 °F]) (%):	1.57

##### Low temperature flexibility:					-13 °F

##### Dimensional stability (maximum movement) (%): 		-0.063

##### Tear strength (kN):						0.5

##### Tensile strength (MPa):					5.7

##### Water vapour transmission (perm):				0.3

### Specified product: ALSAN RS 230 FIELD by SOPREMA.

## SELF-LEVELLING MORTAR

### Two-component polymethyl methacrylate-based (PMMA) liquid membrane is combined with fleece fabric to form a monolithic, self-flashing and self-adhering reinforced field membrane.

### Properties:

##### Density at 73.4 °F (23 °C) (g/ ml):				1.8

##### Viscosity at 77 °F (25 °C):					690

##### Shore A hardness:						91

##### Abrasion resistance 4” disc (mg):				203

### Specified product: ALSAN RS 233 FLASH by SOPREMA.

## FINISH COAT

### Two-component polymethyl methacrylate-based (PMMA) colourless liquid resin infused with aggregates (premixed additive) to which a coloured paste is added and is used as trafficable surface finish.

### Properties:

##### Density at 73.4 °F (23 °C) (g/ml):				1.49

##### Viscosity at 77 °F (25 °C):					3400

##### Shore A hardness:						84

##### Abrasion resistance 4” disc (mg):				133

### Specified product: ALSAN RS 289 TEXTURED BASE by SOPREMA.

## ACCESSORIES

### PRIMER EPOXY

#### Epoxy primer that can be used with polyurethane or epoxy systems to enhance the adhesion of the coating. Also act as a vapour barrier when applied at a minimum thickness of 10 mils.

#### Properties:

### Colour part A:				Clear or translucent white

### Colour part B:				Yellowish

### Viscosity part A (cP):			870

### Viscosity part B (cP):			2150

### Solids by weight (%):			100

### Bond strength (MPa):			> 2

### Specified product: ALSAN FLOOR EP 101 by SOPREMA.

### [OR]

### PMMA PRIMER

#### Translucent cloudy two-component (PMMA) polymethyl methacrylate-based, rapid-curing, primer.

#### Properties:

##### Viscosity at 25 oC (cP):			1200

##### Density at 20 oC (kg/L):			1.02

##### Shore A hardness (ASTM D2240):			97

#### Specified product: ALSAN RS 276 by SOPREMA.

### CRACK SEALANT

#### Adhesive sealant made of moisture cure polyether, with solvent free, low VOC and isocyanates free. Application temperature must be above 0 °C.

#### Product specified: SOPRASEAL SEALANT by SOPREMA.

#### [OR]

#### Two-component polymethyl methacrylate-based (PMMA) liquid membrane is used for filling small cracks, depressions and voids in a substrate prior to applications of resins.

#### Product specified: ALSAN RS PASTE by SOPREMA.

### CATALYST

#### Reactive agent based on dibenzoyl peroxide used to induce curing of resin products during membrane application.

#### Specified product: ALSAN RS CATALYST POWDER by SOPREMA

### FINISH COLOUR ADDITIVE

#### Coloured additive to be added to a polymethyl methacrylate-based (PMMA) clear resin.

#### Specified product: ALSAN RS COLOUR ADDITIVE by SOPREMA

### CLEANER

#### Clear solvent used to clean and reactivate the transition area of in-place rapid-curing.

#### Specified product: ALSAN RS CLEANER by SOPREMA

# EXECUTION

## EXAMINATION AND PREPARATION OF SURFACES

### The following conditions must be met regarding the examination and preparation of surfaces: do not begin any work until surfaces are dry, and free of ice, oil, grease, dirt, excess mortar, or other contaminants. Abrasion of the surface is required to remove contaminants. Do not use liquid products to remove contaminants. Fill in damaged surfaces before application system.

### Chemical surface preparation: Chemical surface preparation (acid etching) is prohibited and will void the manufacturer’s warranty.

### Before waterproofing work begins, the owner’s representative and the membrane contractor’s foreman will inspect and approve substrate condition and ensure that related work has been properly executed. If necessary, a nonconformity notice will be issued to the contractor so that required corrections can be made.

### The decision to begin application of materials constitutes an implicit acceptance of the surface conditions.

### Apply coating materials in accordance with the safety and atmospheric conditions required by the manufacturer of the coating materials or in compliance with municipal, provincial or federal laws and regulations.

### The curing period of the concrete must be at least twenty-eight (28) days with a minimum compressive strength of 24 MPa (3,500 psi); concrete must be free of voids.

### Prepare the concrete to obtain a surface profile (ICRI CSP) of 3 or 4. Use special equipment to achieve such a profile. Shot blasting is recommended.

### The concrete substrate must have a maximum moisture content of 5% (ASTM F2659) or 1.5 kg/100 m²/24 h (ASTM F1869) or an internal relative humidity content of 75% (ASTM F2170).

### Cracks of more than 1.6 mm (1/16 of an inch) must be repaired using crack sealant.

## EXECUTION METHOD

### Waterproofing system work must be executed continuously as surfaces are prepared and weather conditions permit.

### Protect adjacent surfaces against any damage resulting from installation work.

### Installation temperatures must be higher than 59 °F (15 °C) during the installation for the summer version and 23 °F (-5 °C) for the winter version.

## EQUIPMENT

### Maintain equipment and tools clean and in good working order.

### Note: Keep the following paragraph when an epoxy primer is specified.

## APPLICATION OF EPOXY PRIMER

### Mix Part A for at least 2 to 3 minutes and add Part B.

### Mix thoroughly both parts for at least 2 to 3 minutes with a low speed mixer (300 to 450 rpm) and a “Jiffy” type mixing paddle in order to ensure a homogeneous consistency; immediately pour the mix on the substrate.

### Cover the surface using a roller or a flat squeegee to obtain a wet film thickness of 254 micrometres (10 mils).

### Note: The primer must be dry to the touch before applying the waterproofing membrane (maximum time to apply the next coat is 72 hours).

### Note: Keep the following paragraph when a primer made of polymethyl methacrylate (PMMA) is specified.

## APPLICATION OF PRIMER (PMMA)

#### Using a slow-speed mechanical agitator (200 to 400 rpm), thoroughly mix the entire container of resin for two minutes before adding the catalyst.

#### Pour the resin into a second container if a batch mix is made.

#### Add pre-measured catalyst to the resin component according to the amounts indicated in the manufacturer’s Catalyst Mixing Chart. Add the catalyst only to the amount of materials that will be used within the next 10 to 15 minutes.

#### Stir again for two minutes before applying.

#### Apply the resin to the substrate using rollers, brushes or squeegees provided for this purpose.

#### Spread the primer evenly so that the substrate is completely saturated in a single application of 0.4 to 0.5 mm (15 to 20 mils).

## APPLICATION OF THE WATERPROOFING MEMBRANE

### Using a slow-speed mechanical agitator (200 to 400 rpm), thoroughly mix the entire container of resin for two minutes.

### Add the pre-measured catalyst to the resin according to the amounts indicated in the manufacturer’s Catalyst Mixing Chart and mix for two minutes. Add the catalyst only to the amount of materials that will be used within the next 10 to 15 minutes.

### Apply one layer of waterproofing membrane using a roller, a brush or a serrated squeegee on the primer. Thickness must be 1.8 mm (70 mils) when wet.

### Note: The waterproofing membrane layer must be dry before the self-levelling mortar layer is applied. Allow 60 minutes for the summer formula and 90 minutes for the winter formula.

## APPLICATION OF SELF-LEVELLING MORTAR

### Using a slow-speed mechanical agitator (200 to 400 rpm), thoroughly mix the entire container of resin for two minutes.

### Before the addition of the catalyst, add the cement powder while continuing to mix for at least two minutes.

### Add the pre-measured catalyst to the resin according to the amounts indicated in the manufacturer’s Catalyst Mixing Chart and mix for two minutes. Add the catalyst only to the amount of materials that will be used within the next 10 to 15 minutes.

### Apply a layer of the self-levelling mortar on the waterproofing membrane using rollers, brushes or squeegees provided for this purpose. The thickness must be 2 mm (80 mils) when wet.

### Note: The self-levelling mortar layer must be dry before the finishing layer is applied. Allow 60 minutes for the summer formula and 90 minutes for the winter formula.

## APPLICATION OF THE FINISHING LAYER

### Using a slow-speed mechanical agitator (200 to 400 rpm), thoroughly mix the entire container of resin for two minutes before each use so the aggregate mixture is well distributed.

### Add the coloured paste to the colourless resin mixture.

### Add the pre-measured catalyst to the resin according to the amounts indicated in the manufacturer’s Catalyst Mixing Chart and mix for two minutes. Add the catalyst only to the amount of materials that will be used within the next 10 to 15 minutes.

### Apply the finishing resin layer on the self-levelling mortar using rollers, brushes or squeegees provided for this purpose. The thickness must be 0.5 mm (20 mils) when wet.

## INSPECTION

### Inspect all coats of the specified system applied in the liquid state at the end of the work before continuing with the covering work. All imperfections will need to be repaired.

## CLEANING AND PROTECTION

### The applicator shall protect the liquid-applied waterproofing system from damage during its installation. The general contractor shall make provisions to protect the liquid-applied waterproofing during the remainder of the construction period. Repair any damage that may occur after application.

### Remove protective materials after application.

### Clean and remove daily all waste and debris from the worksite to avoid damage and operation disruption.

### Clean tools with a specified cleaner.

### It is recommended to cover the installation as soon as possible.

Note: 	SOPREMA INC. reserves the right to make changes to this specification and associated details without prior notice.

- END OF SECTION -