LIQUID-APPLIED WATERPROOFING 
COATINGS – RETENTION BASINS

ALSAN CIVIL TANK

THIS DOCUMENT PROVIDES TECHNICAL INFORMATION ON MATERIALS AND INSTALLATION METHODS FOR THE ALSAN CIVIL PRODUCT LINE, A COLD-APPLIED WATERPROOFING COATING USED TO WATERPROOF BRIDGES OR ANY OTHER CIVIL ENGINEERING WORK AND THIER ACCESSORIES.

FOR A COMPLETE LIST OF TECHNICAL DATA SHEETS, GUIDE SPECIFICATIONS AND DETAILS PLEASE VISIT OUR WEB SITE WWW.SOPREMA.CA

# GENERAL REQUIREMENTS

## DESCRIPTION

### Supply labour, materials, and equipment required to complete the installation of liquid-applied waterproofing systems for non-potable water retention basins and other permanent or prolonged immersion situations, including surface preparation and accessories.

### The guidelines in this document should be read in conjunction with the product data sheets.

### Cold fluid-applied waterproofing membrane system: ALSAN CIVIL TANK by SOPREMA.

## PERFORMANCE REQUIREMENTS

### Install waterproofing system to accommodate movements of the materials and structural elements in place.

### Ensure the continuity of waterproofing materials and assemblies in accordance with the materials described in the related sections.

## REFERENCES

### ASTM D4060: Standard Test Method for Abrasion Resistance of Organic Coatings by the Taber Abraser.

### ASTM C794: Standard Test Method for Adhesion-in-Peel of Elastomeric Joint Sealants

### ASTM C957: Standard Specification for High-Solids Content, Cold Liquid-Applied Elastomeric Waterproofing Membrane with Integral Wearing Surface

### ASTM C1202: Standard Test Method for Electrical Indication of Concrete’s Ability to Resist Chloride Ion Penetration

### ASTM C1305: Standard Test Method for Crack Bridging Ability of Liquid-Applied Waterproofing Membrane

### ASTM C1522: Standard Test Method for Extensibility After Heat Aging of Cold Liquid-Applied Elastomeric Waterproofing Membranes

### ASTM D412: Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers – Tension

### ASTM D471: Standard Test Method for Rubber Property – Effect of Liquids

### ASTM D2240: Standard Test Method for Rubber Property – Durometer Hardness

### ASTM D4541: Standard Test Method for Pull-Off Strength of Coatings Using Portable Adhesion Testers

### ASTM D5451: Standard Practice for Sampling Using a Trier Sampler

### ASTM E96: Test Methods of Water Vapor Transmission of Materials

## RELATED WORK

### Division [03 00 00] [Concrete]

### Division [05 00 00] [Metal]

### Division [07 00 00] [Thermal and moisture protection]

## SUBMITTALS

### Submit manufacturers’ current product data sheets for the components of specified cold fluid-applied waterproofing membrane.

### Submit samples on rigid substrate for approval by the Owner, Architect, or Engineer specified in Section 01 33 00 ‒ Documents/Samples to Be Submitted.

### Submit shop drawings in accordance with Section 01 33 00 ‒ Documents/Samples to Be Submitted for approval by the Owner, Architect, or Engineer.

## CONTRACTOR QUALIFICATIONS

### Works described in this section must be carried out by a competent contractor certified in waterproofing, employed by a company having the adequate experience and equipment necessary for the works described in this document.

## MANUFACTURER’S REPRESENTATIVE

### The coating materials manufacturer may delegate a representative to visit the work site at commencement of work.

### The contractor shall at all times permit and facilitate jobsite access to any representative of the cold fluid-applied waterproofing materials manufacturer.

## MATERIALS STORAGE

### Handle materials with proper equipment.

### Materials will be delivered to the worksite in the original sealed and undamaged containers.

### The containers must clearly show the product’s and manufacturer’s names as well as the product’s batch number and date of manufacture.

### The delivered materials will be carefully stored and adequately protected according to the manufacturer’s recommendations in order to prevent deterioration caused by humidity, heat, direct sunlight, or any other source.

### Condition sealants at temperatures above 32 °F (0 °C) prior to application and during application. If necessary, conditioning must be done 48 hours before application. Products should be kept away from direct sunlight and heat sources.

## QUALITY ASSURANCE AND ENVIRONMENTAL MANAGEMENT

### Supply cold fluid-applied waterproofing membrane components (including related components and accessories) from one membrane manufacturer to ensure total system compatibility and integrity.

### The coating products manufacturer shall provide proof of ISO 9001 and ISO 14001 certifications.

## WARRANTIES

### The product manufacturer shall issue a written and signed document in the name of the owner, certifying the product will meet all the physical characteristic published by the manufacturer, for a period of 5 years, starting from the date of completion of installation of liquid membranes. No letter amending the manufacturer’s standard warranty will be accepted and the warranty certificate must reflect these requirements.

# PRODUCTS

## BASIS OF DESIGN:

### SOPREMA CANADA, INC.

### 1688 Jean-Berchmans-Michaud

### Drummondville, QC, J2C 8E9

### Web site: www.soprema.ca

## COLD LIQUID-APPLIED WATERPROOFING MEMBRANE

### Description: [Two] [three] component polymethyl methacrylate-based (PMMA) waterproofing [sprayable] liquid membrane flexible at low temperature and is used as a fleeceless waterproofing system. It is used as a waterproofing membrane for bridges, parking decks and other civil engineering structures.

### Specified product: [ALSAN CIVIL 773] [ALSAN CIVIL 773 SP] by SOPREMA.

## COLD LIQUID-APPLIED WATERPROOFING TOPCOAT

### Description: Two-component polymethyl methacrylate-based (PMMA) colourless liquid resin to which a coloured additive is added.

### Specified product: ALSAN CIVIL 370 by SOPREMA

## ACCESSORY MATERIALS

### CRACK SEALANT

#### Description: Two-component crack sealant made of fast-curing, very low viscosity polymethyl methacrylate (PMMA) resin.

#### Specified product: ALSAN CIVIL Z71 by SOPREMA

### PRIMER

#### Description: Two-component crack sealant made of fast-curing, very low viscosity polymethyl methacrylate (PMMA) resin.

#### Specified product: ALSAN CIVIL P70 by SOPREMA

### REACTIVE AGENT

### Description: Reactive agent based on dibenzoyl peroxide used to induce curing of resin products during membrane application.

#### Specified product: ALSAN RS CATALYST POWDER by SOPREMA

#### REINFORCEMENT

#### Description: Non-woven, needle-punched polyester fabric used as fabric reinforcement in two-component cold liquid-applied membrane systems.

#### Specified Product: ALSAN RS FLEECE by SOPREMA

#### COLOR PASTE

#### Description: Coloured additive to be added to a polymethyl methacrylate-based (PMMA) clear liquid resin

#### Specified product: ALSAN RS COLOR ADDITIVE COLORANT [Beige] [Traffic Yellow] [Terra Cotta] [Traffic Red] [Traffic Blue] [Pale Green] [Traffic Green] [Stone Grey] [Pebble Grey] [Light Grey] [Window Grey] [Traffic Grey B] [Signal White] [Traffic Black] by SOPREMA

### CLEANER

#### Description: Clear blenched solvent used to clean and reactivate the transition area of in-place rapid-curing. It can also be used as a solvent to clean up spilled product, tools and equipment.

#### Specified product: ALSAN RS CLEANER by SOPREMA

# EXECUTION

## SURFACE EXAMINATION AND PREPARATION

### The following conditions must be met regarding the examination and preparation of surfaces: do not begin any work until surfaces are smooth, dry, and free of ice, oil, grease, dirt, excess mortar, or other contaminants. Abrasion of the surface is required to remove contaminants. Do not use liquid products to remove contaminants. Fill in damaged surfaces so that they are as smooth as possible.

### The temperature of the substrate must be at least 3 °C above the dew point during the application and curing period. The application temperatures must be between -25 °C to 35 °C (-13 °F to 95 °F). For applications at temperatures below 0 °C, please contact your SOPREMA representative.

### The curing period of the concrete must be at least twenty-eight (28) days with a minimum compressive strength of 24 MPa (3,500 psi); concrete must be free of voids.

### Prepare the concrete to obtain a surface profile (ICRI CSP) of 2. Use special equipment to achieve such a profile. Surface sanding is recommended.

### The concrete substrate must have a maximum moisture content of 5% (ASTM F2659) or 1.5 kg/100 m²/24 h (ASTM F1869) or an internal relative humidity content of 75% (ASTM F2170).

### Remove release agents or other contaminants from the surface of the concrete substrate; use an approved cleaning agent, such as isopropyl alcohol, to remove them completely.

### Prepare steel substrate surfaces according to Standard SSPC-SP10. A pull-out test according to ASTM D4541 should be done to confirm proper adhesion of the primer to the surface.

### Verify the compatibility of all membrane components with curing compounds, coatings, or other materials which are already installed on the surfaces to be treated.

### Before the work begins, the Owner’s Representative and the liquid-applied waterproofing coating contractor’s foreman will inspect and approve substrate condition and ensure that related work has been properly executed. If necessary, a non-compliance notice will be issued to the contractor so that required corrections can be made.

### Beginning the system application implies the acceptance of the concrete surface as satisfactory and ready to receive the waterproofing system.

## EXECUTION METHOD

### Waterproofing works shall be performed on a continuous basis as surface preparation and weather conditions allow.

### Adjoining surfaces shall be protected against any damage that could result from the application works.

### A pull-out test according to ASTM D4541-02 should be done at each 100 m2 (1076 ft2) to confirm proper adhesion of the cold fluid-applied waterproofing coating system to the surface. A minimum adhesion value of 1.4 N/mm2 is required on concrete surfaces.

## EQUIPMENT

### Maintain all equipment and tools in good working order.

## CRACKS REPAIR

### Mix the contents of the crack filler resin container with a mechanical stirrer at low speed (300 rpm) for two minutes before each use and before pouring the resin into a second clean container if you are doing batch mixing.

### Add the specified pre-measured reagent to the resin container and stir for two minutes. Refer to the product data sheet for the quantities of reagent required.

### For cracks up to 3 mm (1/8 in), pour resin over clean, dry cracks and level with a flat squeegee or roller. The resin must be completely dry before applying the primer.

### Any cracks larger than 3 mm (1/8 in) must be reported. After approval by the authority having jurisdiction, fill the cracks with the specified primer previously mixed with silica sand. Refer to the manufacturer for quantities.

## PRIMER APPLICATION

### Mix the content of the specified primer resin container with a mechanical stirrer at low speed (200 to 400 rpm) for two minutes before each use.

### Add the specified pre-measured reagent to the resin container and stir for two minutes. Use and mix only the amount of primer that can be applied within the next 10 to 15 minutes. Refer to the product data sheet for the quantities of reagent required.

### Use a roller or a squeegee to apply a coat of primer at a minimum wet film thickness of 0.54 mm (22 mils) to the dry, clean substrate prepared according to the manufacturer’s recommendations. The primer must be evenly distributed over the surface.

### Wait at least 30 minutes before applying the waterproofing membranes. Make sure the primer is dry.

## REINFORCEMENT INSTALLATION ON UPSTANDS AND DETAILS

### Mix the content of the resin container of the specified liquid-applied waterproofing membrane with a mechanical stirrer at low speed (200 to 400 rpm) for two minutes before each use.

### Add the specified pre-measured reagent to the resin container and stir for two minutes. Use and mix only the amount of resin that can be applied within the next 10 to 15 minutes. Refer to the product data sheet for the quantities of reagent required.

### Using a flat squeegee or a spade roller, apply a layer of the liquid waterproofing membrane with a wet film thickness of 2 mm (80 mils) on the upstand previously coated with primer. The waterproofing membrane must be applied 150 mm (6 in) on the horizontal and 150 mm (6 in) on the vertical of the upstand.

### Install a 305 mm (12 in) strip reinforcement impregnated to saturation onto the waterproofing membrane while still wet.

Note to the specifier: Use this item when the liquid-applied waterproofing membrane is applied manually.

## CONSTRUCTION JOINTS TREATEMENT

### Mix the content of the resin container of the specified liquid-applied waterproofing membrane with a mechanical stirrer at low speed (200 to 400 rpm) for two minutes before each use.

### Add the specified pre-measured reagent to the resin container and stir for two minutes. Use and mix only the amount of resin that can be applied within the next 10 to 15 minutes. Refer to the product data sheet for the quantities of reagent required.

### Using a flat squeegee or a spade roller, apply a layer of the liquid waterproofing membrane with a wet film thickness of 2 mm (80 mils) on the construction joint previously coated with primer. Apply on a width 150 mm (6 in) centered on the joint.

### Install a 150 mm (6 in) strip reinforcement impregnated to saturation onto the waterproofing membrane while still wet.

Note to the specifier: Use this item when liquid-applied waterproofing membrane is applied by roller.

## LIQUID-APPLIED WATERPROOFING MEMBRANE APPLICATION (Roller)

### Mix the content of the resin container of the specified liquid-applied waterproofing membrane with a mechanical stirrer at low speed (200 to 400 rpm) for two minutes before each use.

### Add the specified pre-measured reagent to the resin container and stir for two minutes. Use and mix only the amount of resin that can be applied within the next 10 to 15 minutes. Refer to the product data sheet for the quantities of reagent required.

### Using a flat squeegee or a spade roller, apply a layer of the liquid waterproofing membrane on the substrate previously coated with primer. On the horizontal surfaces, apply one coat with a wet film thickness of 2 mm (80 mils). On the vertical surfaces, apply two coats with a wet film thickness of 1 mm (40 mils). The waterproofing membrane must be evenly distributed over the surface.

### Use a notched gauge to check the thickness of the wet film applied.

### [When the liquid-applied waterproofing membrane is to be installed over several days, overlap the new waterproofing membrane on 50 mm (2 in) over the waterproofing membrane installed the previous day. No preparation is required unless the liquid waterproofing membrane already in place is dirty or contaminated on the edge of the seal. In such a case, clean the edge of the existing waterproofing membrane with specified cleaner before applying the new waterproofing membrane.]

Note to the specifier: Use this item when the liquid-applied waterproofing membrane is applied by spraying.

## LIQUID-APPLIED WATERPROOFING MEMBRANE APPLICATION (Spray)

### Mix the content of the resin container (Part A) of the specified liquid-applied waterproofing membrane with a mechanical stirrer at low speed (200 to 400 rpm) for two minutes before each use.

### Add the specified pre-measured reagent to the resin container (Part A) and stir for two minutes. Refer to the product data sheet for the quantities of reagent required. For applications at temperatures below 0 °C, please contact your SOPREMA representative to find out about the DMPT charter.

### Using a volumetric pump at a ratio of 1:1, spray a layer of the liquid waterproofing membrane on the substrate previously coated with primer. On the horizontal surfaces, apply one coat with a wet film thickness of 2 mm (80 mils). On the vertical surfaces, apply two coats with a wet film thickness of 1 mm (40 mils). The waterproofing membrane must be evenly distributed over the surface.

### Use a notched gauge to check the thickness of the applied wet film.

### [When the liquid-applied waterproofing membrane is to be installed over several days, overlap the new 50 mm (2 in) of waterproofing membrane over the waterproofing membrane installed the previous day. No preparation is required unless the liquid waterproofing membrane already in place is dirty or contaminated on the edge of the seal. In such a case, clean the edge of the existing waterproofing membrane with specified cleaner before applying the new waterproofing membrane.]

Note to the specifier: This topcoat is optional when the membrane is not exposed to UV. It makes it possible to further protect the liquid-applied waterproofing membrane.

## COLOURED TOPCOAT APPLICATION (OPTIONAL)

### Mix the content of the specified topcoat resin container with a mechanical stirrer at low speed (200 to 400 rpm) for two minutes before pouring the coloured paste.

### Mix 1.5 kg (3.3 lb) of coloured paste for each 8.5 kg (18.7 lb) resin container with a mechanical stirrer at low speed (200 to 400 rpm) for two minutes. The colored resin can then be poured into smaller containers if you are doing a batch mix.

### Add the specified premeasured reagent to the amount of resin that can be used within the next 10 to 15 minutes and stir for two minutes. Refer to the product data sheet to know the quantities of reactive agent required. The amount of catalyst added should be based only on the weight of the topcoat resin and not on the entire mixture (resin + synthetic dye).

### Using a roller, brush, or serrated squeegee, apply a coat of the coloured liquid topcoat with a wet film thickness of 0.30 to 0.38 mm (12 to 15 mils) on the waterproofing membrane. The topcoat membrane must be evenly distributed over the surface.

### Use a notched gauge to check the thickness of the applied wet film.

## INSPECTION

### Inspect the entire liquid-applied waterproofing membrane at the end of the works. Any imperfections must be repaired.

## REPAIR

### Repair holes and cracks in the liquid waterproofing membrane.

### Clean the liquid waterproofing membrane before each repair if it is dirty or contaminated.

### Using a flat squeegee or a spade roller, seal the repaired area with an additional coat of liquid-applied waterproofing membrane at a wet film thickness of 2 mm (80 mils) or two coats at a wet film thickness of 40 mils (1 mm), depending on the system.

### If the waterproofing system or part of it has been damaged in any way, cut the damaged waterproofing membrane section.

### Clean the area to be repaired and up to 150 mm (6 in) beyond that area to remove any contaminants.

### If the substrate is exposed or the primer damaged, reapply primer according to the manufacturer’s recommendations.

### Clean the overlap surface with the specified cleaner.

### Apply one coat of liquid-applied waterproofing membrane at a wet film thickness of 2 mm (80 mils) or two coats at a wet film thickness of 1 mm (40 mils).

### Overlap the new liquid waterproofing membrane by 50 mm (2 in) over the existing waterproofing membrane.

## CLEANING AND PROTECTION

### The applicator shall protect the liquid-applied waterproofing system from damage during its installation. The general contractor shall make provisions to protect the liquid-applied waterproofing during the remainder of the construction period. Repair any damage that may occur after application.

### Remove protective materials after application.

### Clean and remove daily all waste and debris from the worksite to avoid damage and operation disruption.

### Clean tools with the specified cleaner. Refer to the manufacturer’s recommendations for spray equipment cleaning.

SOPREMA INC. reserves the right to make changes to this specification and associated details without prior notice.

-END OF SECTION-